Table 1: Selected assay results from 2007 drill holes in the Chrome Mountain and Iron Mountain West areas, Stillwater Project. Intersection intervals represent apparent widths. Holes were drilled at inclinations of –45 degrees. Mapping in the areas indicates stratigraphic units are dipping vertically. Au = Gold, Pt = Platinum, Pd = Palladium, ppb = parts per billion (1000 ppb = 1 gram per tonne).

| 2007 Chrome Mountain Drill Holes |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Hole Number | From (feet) | To (feet) | Interval (feet) | Interval (meters) | Au (ppb) | Pt (ppb) | Pd (ppb) | Au+Pt+Pd (ppb) | Pt/Pd |
| CM2007-01 | 26 | 426 | 400 | 121.9 | 9 | 269 | 236 | 513 | 1.14 |
| includes | 50 | 54 | 4 | 1.2 | 6 | 1660 | 818 | 2484 | 2.03 |
| includes | 78 | 79 | 1 | 0.3 | 108 | 940 | 3880 | 4928 | 0.24 |
| includes | 198 | 200 | 2 | 0.6 | 41 | 1460 | 1360 | 2861 | 1.07 |
| includes | 205 | 206 | 1 | 0.3 | 33 | 590 | 2510 | 3133 | 0.24 |
| includes | 242 | 243 | 1 | 0.3 | 42 | 430 | 1800 | 2272 | 0.24 |
| includes | 390 | 398 | 8 | 2.4 | 26 | 600 | 457 | 1083 | 1.31 |
| CM2007-02 | 44 | 359 | 315 | 96.0 | 31 | 368 | 562 | 961 | 0.65 |
| includes | 79 | 243 | 164 | 50.0 | 56 | 493 | 919 | 1468 | 0.54 |
| includes | 127 | 187 | 60 | 18.3 | 108 | 724 | 1585 | 2418 | 0.46 |
| includes | 139 | 140 | 1 | 0.3 | 172 | 1800 | 2970 | 4942 | 0.61 |
| includes | 150 | 151 | 1 | 0.3 | 226 | 2300 | 5390 | 7916 | 0.43 |
| includes | 219 | 220 | 1 | 0.3 | 97 | 1550 | 2040 | 3687 | 0.76 |
| CM2007-03 | 0 | 156 | 156 | 47.5 | 127 | 306 | 441 | 873 | 0.69 |
| includes | 34 | 138 | 104 | 31.7 | 133 | 359 | 519 | 1011 | 0.69 |
| includes | 133 | 137 | 4 | 1.2 | 173 | 1170 | 1382 | 2725 | 0.85 |
| Hole abandoned @ 156' |  |  |  |  |  |  |  |
| CM2007-04 | 5 | 764 | 759 | 231.3 | 55 | 271 | 371 | 696 | 0.73 |
| includes | 5 | 388 | 383 | 116.7 | 94 | 361 | 568 | 1022 | 0.64 |
| includes | 5 | 62 | 57 | 17.4 | 146 | 398 | 520 | 1065 | 0.76 |
| includes | 71 | 73 | 2 | 0.6 | 76 | 650 | 786 | 1511 | 0.83 |
| includes | 146 | 147 | 1 | 0.3 | 152 | 2130 | 5330 | 7612 | 0.40 |
| includes | 255 | 256 | 1 | 0.3 | 397 | 1650 | 4460 | 6507 | 0.37 |
| includes | 289 | 290 | 1 | 0.3 | 749 | 4370 | 6790 | 11909 | 0.64 |
| includes | 304 | 308 | 4 | 1.2 | 249 | 1430 | 3160 | 4839 | 0.45 |
| includes | 356 | 372 | 16 | 4.9 | 168 | 483 | 316 | 966 | 1.53 |
| includes | 580 | 584 | 4 | 1.2 | 106 | 2880 | 3270 | 6256 | 0.88 |
| CM2007-05 | 212 | 679 | 467 | 142.3 | 49 | 172 | 288 | 509 | 0.60 |
| includes | 309 | 321 | 12 | 3.7 | 134 | 470 | 542 | 1147 | 0.87 |
| includes | 400 | 406 | 6 | 1.8 | 97 | 290 | 1123 | 1510 | 0.26 |
| includes | 546 | 554 | 8 | 2.4 | 144 | 396 | 746 | 1285 | 0.53 |
| includes | 638 | 646 | 8 | 2.4 | 12 | 420 | 1045 | 1477 | 0.40 |
| CM2007-06 | 29 | 284 | 255 | 77.7 | 75 | 211 | 262 | 549 | 0.81 |
| includes | 29 | 48 | 19 | 5.8 | 64 | 305 | 1107 | 1476 | 0.28 |
| includes | 36 | 37 | 1 | 0.3 | 181 | 1080 | 4730 | 5991 | 0.23 |
| includes | 72 | 76 | 4 | 1.2 | 47 | 420 | 817 | 1284 | 0.51 |
| includes | 156 | 204 | 48 | 14.6 | 143 | 389 | 260 | 792 | 1.50 |
| CM2007-07 | 5 | 715 | 710 | 216.4 | 53 | 158 | 324 | 534 | 0.49 |
| includes | 116 | 120 | 4 | 1.2 | 41 | 290 | 1390 | 1721 | 0.21 |
| includes | 142 | 146 | 4 | 1.2 | 67 | 550 | 1560 | 2177 | 0.35 |
| includes | 174 | 182 | 8 | 2.4 | 114 | 275 | 853 | 1241 | 0.32 |
| includes | 224 | 236 | 12 | 3.7 | 103 | 348 | 1486 | 1938 | 0.23 |
| includes | 224 | 230 | 6 | 1.8 | 133 | 517 | 2303 | 2953 | 0.22 |
| includes | 254 | 262 | 8 | 2.4 | 56 | 323 | 942 | 1320 | 0.34 |
| includes | 270 | 272 | 2 | 0.6 | 98 | 260 | 758 | 1116 | 0.34 |
| includes | 282 | 286 | 4 | 1.2 | 233 | 610 | 690 | 1533 | 0.88 |
| includes | 488 | 518 | 30 | 9.1 | 88 | 181 | 342 | 611 | 0.53 |
| includes | 536 | 542 | 6 | 1.8 | 107 | 355 | 739 | 1202 | 0.48 |
| includes | 546 | 566 | 20 | 6.1 | 113 | 521 | 1700 | 2333 | 0.31 |
| includes | 554 | 555 | 1 | 0.3 | 179 | 1090 | 4240 | 5509 | 0.26 |
| includes | 611 | 623 | 12 | 3.7 | 77 | 273 | 822 | 1172 | 0.33 |
| includes | 651 | 667 | 16 | 4.9 | 156 | 453 | 990 | 1598 | 0.46 |
| CM2007-08 | 130 | 540 | 410 | 125.0 | 95 | 280 | 379 | 754 | 0.74 |
| includes | 130 | 155 | 25 | 7.6 | 147 | 465 | 616 | 1228 | 0.75 |
| includes | 141 | 142 | 1 | 0.3 | 319 | 1340 | 1590 | 3249 | 0.84 |
| includes | 283 | 326 | 43 | 13.1 | 105 | 380 | 621 | 1106 | 0.61 |
| includes | 302 | 306 | 4 | 1.2 | 126 | 660 | 1260 | 2046 | 0.52 |
| includes | 342 | 472 | 130 | 39.6 | 123 | 392 | 566 | 1081 | 0.69 |
| includes | 421.5 | 422.1 | 0.6 | 0.2 | 90 | 2030 | 4250 | 6370 | 0.48 |
| CM2007-09 | 12 | 75 | 63 | 19.2 | 104 | 366 | 596 | 1066 | 0.61 |
| includes | 27 | 47 | 20 | 6.1 | 211 | 410 | 899 | 1520 | 0.46 |
| includes | 43 | 47 | 4 | 1.2 | 228 | 730 | 1980 | 2938 | 0.37 |
| includes | 51 | 75 | 24 | 7.3 | 60 | 480 | 628 | 1168 | 0.76 |
| Hole abandoned @ 75' |  |  |  |  |  |  |  |  |
| CM2007-10 | 11 | 355 | 344 | 104.9 | 50 | 265 | 371 | 686 | 0.72 |
| includes | 35 | 58 | 23 | 7.0 | 133 | 457 | 924 | 1514 | 0.49 |
| includes | 52 | 58 | 6 | 1.8 | 181 | 847 | 1982 | 3009 | 0.43 |
| includes | 67 | 127 | 60 | 18.3 | 57 | 389 | 507 | 953 | 0.77 |
| includes | 83 | 87 | 4 | 1.2 | 71 | 940 | 1280 | 2291 | 0.73 |
| includes | 131 | 147 | 16 | 4.9 | 30 | 600 | 771 | 1401 | 0.78 |
| includes | 191 | 207 | 16 | 4.9 | 12 | 320 | 499 | 831 | 0.64 |
| includes | 303 | 343 | 40 | 12.2 | 85 | 383 | 525 | 993 | 0.73 |